EURAMET.QM-S18

Determination of gold content in metal alloys

Supplementary Comparison

Study Protocol

[September 2026]

Aida Jotanović

Institute of metrology of Bosnia and Herzegovina

INTRODUCTION

The need for international comparisons in gold alloy analysis has been expressed by several national metrology institutes (NMIs) due to the critical importance of accurate gold determination, particularly in the jewellery industry and monetary reserves. Gold purity certification is essential for trade, investment, and regulatory compliance, requiring reliable measurement methods supported by metrological traceability.

As a follow-up to the recently completed  EURAMET TCMC Project 1455: "Comparison on Determination of Gold Content in Alloy," which confirmed good comparability among different analytical methods, the Institute for Metrology of Bosnia and Herzegovina proposes organizing a EURAMET supplementary comparison for the determination of gold in metal alloys. This follow-up aims to further demonstrate participants’ competence and verify their measurement capabilities in gold analysis.

Within the current IAWG plan, this sample matrix falls under the matrix challenge “Metals, alloys, and difficult to dissolve metals” for the analytes in the group of “Transition elements”.

Although it was conceived to be a regional comparison, it is open to other participants of the MRA throughout all RMOs.

TIMELINE

The following table lists the timeline for the proposed study.

Table 1. Proposed schedule

| Date | Action |
| --- | --- |
| December 2025 | Sample Preparation |
| April-July 2026 | Homogeneity and Stability Testing |
| September 2026 | Call for participation |
| November 2026 | Deadline for registration |
| December 2026 | Sample Distribution |
| November 2027 | Deadline for Submission of Results |
| February 2028 | Preliminary Discussion of Results |

MEASURAND

This comparison is designed to focus on gold mass fraction as a mandatory measurand, aiming to determine its total content in alloys at two different mass fraction levels. The expected mass fractions of gold are presented in Table 2.

Table 2. Measurands and expected mass fraction range

| Sample | Measurand nominal value of Au mass fraction (mg/g) |
| --- | --- |
| Au-10 | 100 - 200 |
| Au-99 | 950 - 999 |

STUDY MATERIALS

Approximately 30 g of study material for each mass fraction level was prepared in the form of wire by an experienced goldsmith from Bosnia and Herzegovina. The wire was cut into individual pieces of approximately 1 g each and packaged separately in plastic bags.

Recommended Minimum Sample Amount

The recommended minimum test portion required for analysis is 0.2 g, ensuring compliance with the requirements of the applied analytical method.

Homogeneity Assessment of Study Material

The homogeneity study was performed under repeatability conditions using the gravimetric cupellation method for the determination of gold content. From each wire specimen, two independent test portions were analysed, and the results were evaluated using one-way analysis of variance (ANOVA) at 95 % confidence level to assess between-unit homogeneity.

The results confirmed that the study material was sufficiently homogeneous. The results are summarized in Table 3.

Table 3. Homogeneity assessment

| Measurand | F | Fcrit | ubb (mg/g) | ubb (%) | p | Technique |
| --- | --- | --- | --- | --- | --- | --- |
| Au-10 | 2.15 | 4.39 | 0.28 | 0.27 | 0.19 | gravimetric fire assay |
| Au-99 | 3.63 | 4.39 | 0.25 | 0.03 | 0.07 | gravimetric fire assay |

Based on the ANOVA results and the low estimated between-unit standard deviations, both Au-10 and Au-99 materials were considered sufficiently homogeneous for their intended purpose.

Stability Assessment of Study Material

Considering the inherent chemical and physical stability of precious metal alloys, and their demonstrated resistance to compositional changes under appropriate storage conditions, no stability study was performed.

Available Calibration Materials

Metrological traceability of results to the SI may be established by participants using a direct realization via primary method, certified reference materials (CRMs) from an NMI/DI with the required CMC claims, or by preparing their own calibration standards using commercially available high-purity materials, whose purity should be determined in house or by another NMI/DI with the necessary CMC claims.

The following is a list of CRMs available for use in this study, as known to the study coordinator at the time of protocol preparation:

| CRM | Traceability provider | Description |
| --- | --- | --- |
| SRM 3121 | NIST | Primary calibration solution for the quantitative determination of gold |
| Commercially available high purity Au by various producer | NRC | HiPu-8: Mechanism for measurement service delivery: Customer service; GD-MS-200; delivery only to other NMIs |

INSTRUCTIONS AND SAMPLE DISTRIBUTION

The samples will be distributed via ordinary postal service, as precious metals are highly stable and do not require any special conditions during transport.

RESULTS

The results, obtained from a minimum of four independent replicates, should be submitted to the coordinator by the previously agreed deadline using the provided reporting template.

All participants must include following:

- Final results and uncertainty budget, reported in mg/g based on at least four independent replicate measurements;

- A detailed description of the sample preparation methods, analytical techniques, calibration approach and any corrections applied. Furthermore, a full uncertainty budget should be reported as part of the results.

HOW FAR THE LIGHT SHINES

Successful participation in this supplementary comparison demonstrates the capability of NMIs and DIs to determine the mass fraction of gold in metal alloys, providing evidence of their measurement competence and methodological reliability.

The comparison is intended to support existing and future Calibration and Measurement Capabilities (CMCs) for the determination of the mass fraction of gold in metal alloys by primary measurement methods. The supported measurement scope covers homogeneous metal alloy matrices within the mass fraction range represented by the comparison artefacts (100 mg/g to 990 mg/g Au).

According to the IAWG Core Capability Matrix, the comparison material belongs to the Metal Alloys matrix category and supports CMC claims for gold (transition elements) at the mg/g level under the CIPM MRA.

CONTACT DETAILS

Aida Jotanović

Institute of metrology of Bosnia and Herzegovina

+387 61 841 667; +387 33 568 925

aida.jotanovic@met.gov.ba